Contact and volumetric heating of potato starch in a closed mould

Jan Skočilas,a Rudolf Žitný.a

aCzech Technical University in Prague, Faculty of Mechanical Engineering, 166 07, Prague 6, Technická 4. phone:+420 224 352 719,fax: +420 224 310 292,

jan.skocilas@fs.cvut.cz, rudofl.zitny@fs.cvut.cz

Summary:

Processes of thermal treatment of starch-based materials for biologically degradable packaging products are analyzed. The contribution describes experiments on thermal forming of potato starch based water suspensions in a closed mold at elevated pressures and temperatures up to 200 0C. Liquid samples are heated in laboratory molds either by contact with the heating plates or by direct ohmic heating. The time course of temperatures as well as the sample expansion were detected by a network of thermocouples and compared with the recorded pressure inside the mold. Results show some disadvantages of the direct ohmic heating and microwave heating (poor contact electric resistance and an absence of crust, worsening mechanical properties of the prepared samples). The experimentally observed fact, that the radial temperatures are almost uniform, does not correspond to the idea of a radial flow of liquid core, suggested by Zitny (2002) and therefore is substituted by a model of expanding foam. The foam behavior is modeled according to the idea of expanding spherical bubble, filled by a saturated steam, Fan (1999). Parameters of model are identified by comparing the theoretical predictions with the experimental data (temperature profiles and expansion rate).

Keywords: starch, thermal forming, mould filling, expansion

### Nomenclature

A	hear transfer area [m2]

B	evaporation constant [-]

c	heat capacity [J.kg-1.K-1]

F	fluidity

H	sample thickness [m]

h	liquid layer thickness [m]

hi	heat transfer coefficient [W.m-2.K-1]

hc	overall heat transfer coefficient [W.m-2.K-1]

K	consistency coefficient [Pa.sn]

M,Mf,Mb sample mass, free and bound water mass [kg]

Nb	number of bubbles [-]

n	flow index [-]

p	pressure [bar]

r	evaporation heat [J.kg-1]

R	gas constant [J.mol-1.K-1]

Rb	bubble radius [m]

t	time [s]

T	sample temperature [0C]

Tw	wall temperature [0C]

V	volume [m3]

- evaporation coefficient [s-1]

- permeability [kg.s-1.bar-1]

1. Introduction

Technology of thermal forming of starch suspension enables to replace the plastic product by biodegradable materials. One of the drawbacks of this method is a long process time, which could be shortened by ohmic or microwave heating.

Several interesting phenomena were observed when a thin sample of concentrated starch suspension was heated in a closed mold at a constant wall temperature, Zitny (2002): 1. Temperature increase at a center of the heated sample needn’t be monotonous (even a temporary temperature decrease was observed). 2. Even if the mold is vented along its perimeter an elevated pressure was recorded at a surface of heated sample. 3. Heated sample expands significantly inside the mold increasing initial volume almost three times.

Possible explanation of the strange temperature phenomena based upon the concept of compact crust, porous crumb and flowing core (CCC model), was presented previously, Žitný et al. (2002a,b). The CCC model predicted nonuniform pressure profile along the sample surface (assuming atmospheric pressure at a perimeter) and also non-uniform temperature profiles, closely related to pressure of escaping steam. New experiments make this hypothesis questionable, Žitný et al. (2006), because measured longitudinal temperature profiles were almost uniform during the second stage of free water evaporation. Therefore the rather complicated CCC-model was replaced by a simple integral model, calculating only the mean temperature, mean pressure, and the mean water content as a function of time. Basic assumption that the temperature is controlled by pressure of steam was preserved, but the strict relationship between the pressure and the mass flowrate of escaping steam, taking into account porosity and thickness of crumb evolution, was relaxed. Thus it is possible to take into account also another sources of hydraulic resistance, first of all additional flow resistance of vents filled by the expanding sample.

The previous integral model is useful for scale up, for temperature and pressure estimation, but not for description of expansion. Similar model of bread baking was suggested by Zanoni et al.(1994), (1995). The model assumed a moving crust/crumb boundary; nevertheless, the expansion of the sample was described by quite empirical equations without temperature history consideration. Gan et al. (1995) and Fan et al. (1999) used the concept of expanding foam. The foam is formed by starch matrix, liquid film and gas bubbles and dough expansion was considered to be related to bubbles expansion at the early phase of baking. Zhang et al. (2005) also described bread baking, but used a complicated viscoelastic rheological constitutive equation necessitating purely numerical 3D solution. Baking takes place at atmospheric pressure and this is the fundamental difference from the thermal pressure forming in a closed mold. An attempt to model the expansion of sample at elevated pressure was presented by Žitný et al. (2006) assuming a squeezing flow of suspension in the liquid core (the concept of CCC structure was also adopted). Disadvantage of this approach is prediction of strongly nonuniform lateral pressure profile and also prediction of porous structure that does not conform to observations.

2. Integral model

It seems to be obvious, that the hypothesis of temperature controlled by pressure inside the mould is in contradiction with observations (uniform longitudinal temperature profile). This is not quite so. The discrepancies concerning more or less uniform longitudinal temperature profile were explained by the effect of vents blocked by expanded material. The blocking effect was manifested by significant pressure peaks recorded soon after the moment, when the expanding sample arrived to the venting holes. In this case the pressure (and therefore also the temperature) inside the mold must be elevated and almost uniform. The incomplete filling of the venting holes explains also a poor repeatability of results. On the other hand the experiments carried out with a smaller amount of suspension, such, that the mold was not completely filled by the expanded material, exhibited also a significant initial pressure peak during expansion and a mild elevation of pressure during the subsequent phase of free water evaporation. This observation can be explained by the model of expanding foam. The temperature profile evolution concept is shown in the fig.1. The process is distinguished into four stages. First, third and fourth stage are without changes according to Žitný et al. (2006).

Fig. 1 Temperature profile of the sample during process

The first stage is characterized by a linear temperature rising up to 100°C, and no phase or mass changes of the heated sample.

.						           (1)

Mass of sample M0, contact surface A as well as the heat transfer coefficient hI are assumed constant.

At the second stage, when the temperature exceeds 100°C, the sample expands due to growing bubbles. In the end of the second stage, the sample fills whole mould. Description of this process requires to identify the number of bubbles (from porosity experiments), the initial bubble radius and rheological properties of the expanding sample. We assume that water is entrapped inside impermeable bubbles and that the whole heat transferred into the sample is consumed by evaporation of free water inside the bubbles. The expansion rate of sample (in fact the expansion rate of a bubble in a liquid matrix dRb/dt) is determined by the flow properties of suspension, characterized by the flow  index n and by the consistency K, see Fan et al. (1999).

, 								(2)

where the parameter F is a fluidity coefficient of the liquid matrix

.							(3)

As soon as the contact surface A as well as the sample mass (or the mass of evaporated water Mv) are no more constant, the enthalpy balance of the whole sample (total enthalpy H)

(4)

must be completed by additional equations, namely by the flow equation of bubble (2), together with the pressure-temperature equilibrium relationship and the state equation of ideal gas. In this way the time derivative dMv/dt can be eliminated, giving

,            (5)

where

(6)

This Eq.(5) can be considered as an equation for temperature, because the pressure p can expressed in terms of temperature using Clausius Clapeyron equation

,								(7)

and the contact surface A(t) follows directly from the bubble radius Rb and the number of bubbles Nb.

The third stage describes the state when the expansion is completed (therefore the heat transfer surface Amax is constant). The porous structure is getting permeable, and therefore evaporated steam flows out of the mold. Assuming that the mass flowrate of escaping steam is directly proportional to the overpressure p-pa (coefficient of proportionality is an empirical parameter ( of model), the enthalpy balance can formulated by equation.

(8)

where

(9)

and

, , 	(10-12)

The fourth stage of heating is based on the assumption that the amount of the evaporated steam is proportional to the amount of bound water

(13)

and the enthalpy balance takes the form

, 	      (14)

where

.	           (15)

3. Experimental setup

There have been two apparatuses applied at presented work, the one for the contact and the second for the volumetric heating. The first apparatus consists of two heated plates that form close rectangular mould 270x200 mm with the adjustable thickness of 2,4 and 8 mm. The technology of thermal forming of the starch suspension at elevated pressure has been used at this apparatus. Sample was poured onto the preheated lower plated and mould was closed. The pressure of evaporated steam, temperature of sample and plates and sample expansion are measured continuously by pressure transducer TDT 432–H–M18–17–15/46 Dynisco located in the middle of the upper plate and by a set of thermocouples. The needle thermocouples were located in the middle of the sample for measuring temperature and inside the mould for expansion measurement. All data were recorded by the data logger Agilent and stored in PC. The scheme of the apparatus is shown in fig.2.

Fig. 2 Scheme of apparatus for thermal forming of starch suspension

The second simple apparatus consists of a plastic body with a cylindrical cavity and two stainless steel electrodes one at the top and the second at bottom of the cavity. The sample temperature is measured by a needle thermocouple. The electrodes are fed by a laboratory power source 50 Hz with maximum power 15 kW. The power, voltage and current are measure by the power meter Tectra. The scheme of the apparatus is shown in fig 3.

Fig. 3 Scheme of the direct ohmic heating cell

4. Experiments and results

4.1	Material properties of starch suspension and produced samples

The basic thermodynamic properties of the pure starch were adapted from Zanoni et al. (1991), Wang and Hayakawa (1993), Maroulis et al (1990) studies with temperature dependency. The properties of the starch-water suspension were determined by addition rule. Only the density was observed experimentally at 20°C for different mass fraction of the starch. The relative mass fraction of the bound water was evaluated from sorption isotherms presented by Lind and Rask (1991).

The porosity and number of bubbles were determined from photographs of the slice, see fig.4. The boundaries of the pores were sharpened by paint. Then the photographs were processed by program for determining the area of the specific color and for counting of closed regions. The number of  bubbles in the whole sample was evaluated from number of pores at specific slice and than recalculated to the whole volume assuming isotropy of bubbles.

Fig. 4 The photograph of the sample slice

4.2 Contact heating

The aim of measurement was to get the temperature and pressure time profiles and the expansion rate of the starch material for two thicknesses of sample (distance of heating plates) 4 and 8 mm. The time courses of temperature are compared with the mathematical model, see Figs.5 and 6, presenting the temperature and pressure profiles for the 4 mm thickness and for different masses of sample (the small amount of starch corresponds to the case, when the mold is not completely filled).

Majority of experiments carried out with thick samples (thickness 8 mm) exhibited a poor reproducibility of temperature and pressure profiles. We suppose that the problem is caused by the non-uniform hydraulic resistance of vented gaps at the periphery of the mould, when the sample fills the whole space of the cavity and blocks the vents. The evaporated steam passes through the partially obstructed venting gaps with increased hydraulic resistance affecting the pressure and temperature inside the mould, see Fig.8. The results with samples, that do not fill the whole mould, exhibited much better repeatability, Fig.7.

The essential feature of thermal forming technology is a considerable volumetric expansion and an elevated pressure inside the mould during heating. After pouring the sample onto the lower plate and closing the mould the sample expands immediately. End of expansion is marked by vertical lines in Figs. 5, 6, 7 and 8. The expansion rate was measured by a network of needle thermocouples located inside the mould (the measuring junctions were outside of the sample border). When the periphery of the expanding sample reached a thermocouple, the temperature was changed and this sudden alternation indicated the exact time and place of the sample border. The measured time courses of expansion are shown in Fig.9 for the 4 mm thickness sample and for different mass of the sample 100, 120 and 130 g. The averaged time from closing the mould to expansion is around 50 s for the 4 mm sample.

Fig. 9 Expansion rate of the 4 mm sample

Expansion rate of the 8 mm sample is shown in the Fig.10 only for one sample mass 150 g. The average expansion time is around 130 s for 8 mm sample.

Fig. 10 Expansion rate of the 8 mm sample

The mathematical model presented in the chapter 2 (integral model) was implemented into the program FEMINA, which involves optimization procedures. The model parameters were identified using experimental data by this program. Values of five parameter are presented in table 1, the other two parameters were assumed constant – initial radius of the bubble Rb0 = 0.2 mm and flow index n = 0.672.

Tab.1 Parameters of the model

| Parameter | 4 mm * | 4 mm | 8 mm * | 8 mm |
| --- | --- | --- | --- | --- |
| ( *10-8 | 0.65 | 0.65 | 0.80 | 0.30 |
| h1 | 0.80 | 0.80 | 0.80 | 0.80 |
| h2 | 0.80 | 0.35 | 0.80 | 0.35 |
| h3 | 0.67 | 0.50 | 0.80 | 1.40 |
| h4 | 0.75 | 0.57 | 0.85 | 1.50 |

* - sample not fill the mould

4.3 Direct ohmic heating

The following figure 11 shows the result of preliminary experiment with the direct ohmic heating using the ohmic heating cell. The power, voltage, current and temperature were measured, whereas the presented conductivity of the sample was computed. The mass of sample was 48 g, mass fraction of the starch 50 %, and the 0.5 g of salt was added for improving conductivity. The maximum value of electrical power applied into the sample was not higher than 140W.

Resulting temperature time course shown in Fig.11 demonstrates the fact, that the whole process of thermal forming cannot be completed using the direct heating only. The reason is a significant decrease of electric conductivity of partly dried sample. Temperature of the heated sample only slightly exceeded 100 °C, and the structure of the produced sample was gelatinous, without any crust or a fixed porous structure (nevertheless the bubbles inside the sample were noticeable). Thus the ohmic heating could be applicable only at the first stage of the process for a quick heating up to 100°C and semidrying with lower power consumption compared to conduction heating. The drawbacks are the decreasing the sample conductivity during drying and the electrochemical corrosion of the electrodes.

Fig. 11 Temperature and the conductivity of ohmic heated sample.

5. Conclusion

The experiments were oriented first of all to the effect of venting (and obstruction of venting holes by expanding starch) upon the temperature and pressure profile. This effect was identified as a cause of a bad reproducibility of results (temperature and pressure time profiles).

The expansion rate for different sample mass was examined by experiments. The value of expansion rate for 4 mm thickness sample is 3.2 cm3.s-1 and for 8 mm thickness sample is 2.2 cm3.s-1.

The ohmic heating is suitable only for the initial stages of heating as soon as the sample contains sufficient amount of water. The drawback of the direct ohmic process is low conductivity of sample and a bad structure of the sample (absence of crust).

### Acknowledgement

This research has been subsidized by Grant Agency of Czech Republic 101/06/0535

6. References

- Fan J., Mitchell J.R., Blanshard J.M.V. (1994): A computer simulation of the dynamics of bubble growth and shrinkage during extrudate expansion. Journal of Food Engineering, 23, 337-356

- Gan Z., Ellis P.R., Schofield J.D. (1995): Mini rewiev gas cell stabilization and gas retention in wheat bread dough. Journal of Cereal Science, 21, 215-230

- Lind I., Rask C. (1991): Sorption isotherms of mixed meat, dough and bread crust. Journal of Food Engineering, 14, 303-315

- Maroulis Z.B., Drouzas A.E., Saravacos G.D. (1990): Modeling of thermal conductivity of granular starches. Journal of Food Engineering, 11, 255-271

- Ramesh N.S., Rasmussen D.H., Campbell G.A.: Numerical and experimental studies of bubble growth during microcellular foaming process. Polymer Engineering and Science, (1991), vol.3, No.23, pp. 1657-1664

- Skočilas, J., Žitný, R. Thermal Pressure Forming of Food Materials In: 17th International Congress of Chemical and Process Engineering [CD-ROM]. Prague: Czech Society of Chemical Engineering, 2006, s. 1-9. ISBN 80-86059-45-6

- Wang W.Ch., Sastry S.K. (1997): Starch gelatinisation in ohmic heating. Journal of Food Engineering, 34, 225-242

- Wang J.,Hayakawa K. (1993): Thermal conductivities of starch gels at high temperatures influenced by moisture. Journal of Dood Science, 58(2)

- Wu Y., Irudayaraj J. (1996): Analysis of heat, mass and pressure transfer in starch based food systems. Journal of Food Engineering, 29, 399-414

- Zanoni B., Smaldone D., Schiraldi A. (1991): Starch gelatinization in chemically leavened bread baking. Journal of Food Science, 56(6), pp.1702

- Zanoni B., Pierucci S., Peri D. (1994): Study of the bread baking process-II. Mathematical modeling. Journal of Food Engineering 23, 321-336

- Zanoni B., Peri C., Bruno D. (1995): Modelling of starch gelatinisation kinetics of bread crumb during baking. Lebensmittel- Wissenschaft und Technologie, 28(3), 314-318

- Zhang J., Datta A.K. (2005): Mathematical modeling of bread baking process. Journal of Food Engineering, 75, 78-89.

- Zhang J. (2003): Multiphase heat and mass transfer with large deformation in porous media. PhD Thesis.

- Žitný R., Šesták J., Tsiapouris A., Linke L. (2002a): Modelling of thermal pressure forming of starch-based materials. Journal of Food Engineering, 52, 375-385

- Žitný R., Šesták J., Tsiapouris A., Linke L. (2002b): Thermal pressure forming: A simplified Thermodynamical Model, Proceedings of the Twelfth International Heat Transfer Conference, Grenoble, August 18-23, 2002

- Žitný R. (2005): FEMINA User manual. http://www.fsid.cvut.cz/~zitny/feminstal.exe

- Žitný, R. - Šesták, J. - Skočilas, J. Combined Thermal Pressure Forming of Starch Suspension In: 13th International Heat Transfer Conference [CD-ROM]. Sydney: Begell House Inc., 2006, s. 1-12. ISBN 1-56700-226-9.

# Text boxes

Fig. 8 Temperature and pressure inside the mould, 8 mm thickness sample, mass fraction of the starch 0.52, mass of sample 250 g, sample filled the mould

Fig. 7 Temperature and pressure inside the mould, 8 mm thickness sample, mass fraction of the starch 0.52, mass of sample 250 g, sample did not fill the mould

Fig. 6 Temperature and pressure inside the mould, 4 mm thickness sample, mass fraction of the starch 0.52, mass of sample 150 g, sample fills the mould completely

Fig. 5 Temperature and pressure inside the mould, 4 mm thickness sample, mass fraction of the starch 0.52, mass of sample 50 g, mould is not completely filled.

perforation of bubbles

expansion stops